Purpose:

Define the process for analyzing Bright, Semi-Bright, Particle, & HP Armor Nickel Plating Bath samples.

Definitions:

DI – Deionized or Reverse Osmosis (RO)

g – Grams

g/l – Grams  per Liter

ml - milliliter

oz/gal – Ounces per Gallon

ppm – Parts Per Million

Procedure:

* See WI-8.2.4-13 Lab Solutions & Indicator Preparation for Make-Up Instructions

A customer specific spreadsheet can be used in place of the listed worksheet

Nickel Metal:

- Pipette 1ml of sample into a suitable 150ml beaker

- Add approximately 25ml of DI water to the beaker

- Add approximately 10ml of 26° Ammonium Hydroxide to the beaker (solution will turn blue)

- Add a stir bar, place on a magnetic stir plate, and begin mixing

- Add a pinch (approximately 0.5 – 1 gram) of Murexide Indicator* to the beaker.  The solution should turn brown.

- Titrate against 0.1M EDTA until the solution turns to a deep purple

- Record the ml EDTA titrated on the Nickel Plating Baths Analysis Worksheet

- Calculate oz/gal Nickel Metal

Calculation:  ml EDTA x M EDTA x 7.85 = oz/gal Nickel Metal

Nickel Chloride:

- Pipette 2ml of sample into a suitable 150ml beaker

- Add approximately 80ml of DI water to the beaker

- Add 5 – 10 drops of 2% Sodium Dichromate Indicator* to the beaker (solution should turn orange)

- Add a stir bar, place on a magnetic stir plate, and begin mixing

- Titrate against 0.1N Silver Nitrate (AgNO3) until a brownish-red color forms

- Record ml AgNO3 titrated on the Nickel Plating Baths Analysis Worksheet

- Calculate oz/gal Nickel Chloride

Calculation: ml Silver Nitrate x N Silver Nitrate x 7.94 = oz/gal Nickel Chloride

Procedure: Continued

Nickel Sulfate:

- Calculate the oz/gal Nickel from Nickel Chloride

Calculation: oz/gal Nickel Chloride x 0.247 = oz/gal Nickel from Nickel Chloride

- Calculate oz/gal Nickel Sulfate

Calculation: (oz/gal Nickel Metal – oz/gal Nickel from Nickel Chloride) / 0.223 = oz/gal Nickel Sulfate

Nickel Sulfamate:

- Calculate the oz/gal Nickel from Nickel Chloride

Calculation: oz/gal Nickel Chloride x 0.247 = oz/gal Nickel from Nickel Chloride

- Calculate oz/gal Nickel Sulfate

Calculation: (oz/gal Nickel Metal – oz/gal Nickel from Nickel Chloride) / 0.234 = oz/gal Nickel Sulfamate

Boric Acid:

- Pipette 2ml of sample bath into a suitable 150ml beaker

- Add approximately 100ml of DI water to the beaker

- Add a stir bar, place on a magnetic stir plate, and begin mixing

- Immerse pH probe into solution and adjust pH to between 3.9 – 4.1 with

  - 0.1N Sulfuric Acid (H2SO4)* if initial pH is higher than 4.0

  - 0.1N Sodium Hydroxide (NaOH) if initial pH is lower than 4.0

- Add approximately 5 grams of Mannitol to the beaker and allow to dissolve

- Titrate against 0.1N Sodium Hydroxide (NaOH) until the pH reaches 6.5

- Record ml NaOH titrated on the Nickel Plating Baths Analysis Worksheet

- Calculate oz/gal Boric Acid

Calculation:  ml NaOH x N NaOH x 4.13 = oz/gal Boric Acid

Procedure: Continued

pH:

Follow TM-12 Determining pH

Surface Tension:

See TM-42 Determining Surface Tension in Liquids

Index:

- Pipette 10ml of sample bath into a 250ml Erlenmeyer flask

- Add approximately 25ml of DI water to the flask

- Add a stir bar, place on a magnetic stir plate, and begin mixing

- Add approximately 20ml of 1:1 Hydrochloric Acid (HCl)* to the flask

- Add approximately 10 drops of Methyl Orange Indicator* to the flask

- Titrate against 0.1N Potassium Bromate/Bromide (KBr)to the solution turns green

- Record the ml KBr titrated on the Nickel Index / Carrier Analysis Worksheet

- Calculate % Index

Calculation:  ml KBr x N KBr x 2.67 = % Index

Carrier:

- Pipette 2ml of sample bath into a 100ml volumetric flask

- Fill the flask to the etch mark with DI water and mix

- Turn on Spectrophotometer, warm up as necessary

Use OSO Cuvette for testing

- Press the “Carrier” icon

- Press “Start” icon – the meter will display “insert cuvette with blank”

- Rinse Cuvette with DI water and then fill with DI water for use as a blank

- Place Cuvette into meter and press “OK”

- After taking the ‘Blank’ reading the meter will display “Insert cuvette with sample ID1”

- Empty the Cuvette, rinse with sample bath, and then fill with sample bath of testing

- Place Cuvette into meter and press “OK”

- Read results at 315 & 285 abs and record on the Nickel Index / Carrier Analysis Worksheet

- Calculate % Brightener / Carrier

Calculation:  (285 abs – 315 abs) x 8.2 = % Brightener / Carrier

Procedure: Continued

ZT Carrier:

- Pipette 10ml of sample bath into a 100ml volumetric flask

- Fill the flask to the etch mark with DI water and mix

- Turn on Spectrophotometer, warm up as necessary

Use OSO Cuvette for testing

- Press the “ZT” icon

- Press “Start” Icon – the meter will display “Insert cuvette with blank”

- Rinse Cuvette with DI water and then fill with DI water for use as a blank

- Place Cuvette into meter and press “OK”

- After taking the ‘Blank’ reading the meter will display “Insert cuvette with sample ID1”

- Empty the Cuvette, rinse with sample bath, and then fill with sample bath of testing

- Place Cuvette into meter and press “OK”

- Read results at 264 & 262 abs and record on the Nickel Index / Carrier Analysis Worksheet

- Calculate % Brightener / Carrier

Calculation:  (264 abs – 262 abs) x 37.5 = % Brightener / Carrier

Leveler:

See TM-160 Determining % Nickel Leveler – HPLC

Procedure: Continued

HP Armor – Particle Nickel Solids:

- Pipette 10ml of a thoroughly mixed, warm bath sample into a clean Kocour tube

- Pipette 15ml of 140 – 160 °F DI water into the Kocour tube

- Stopper the Kocour tube and mix thoroughly for 30 seconds

- Place Kocour tube in a Centrifuge

- Add approximately 25ml of water to a 2nd Kocour tube (will be used as a counterbalance)

- Place the Kocour tube (counterbalance) with 25ml water opposite of the sample tube (step #4)

- Spin sample and counterbalance for 5 minutes

- Remove the sample tube and read the solids leveler (in oz/gal)

- Calculate the Solids

Calculation:  Reading x 7.49 = g/l Solids

Note:  The above calculation has been condensed.  For reference the full calculation is as follows:

(Reading / 3.785) x 28.35 = g/l Solids

References:

TM-12 Determining pH

TM-42 Determining Surface Tension in Liquids

TM-160 Determining % Nickel Leveler – HPLC

Records:

Plating Bath Reports